Table S4. Previous experimental partitioning D values for schreibersite/solid metal partitioning.

Element (schreibersite)/Fe-Ni

Ni 1.0

As 0.16

Mo 3.9

Pd 0.78

Sb 0.045

Au 0.017

Data from Jones et al. (1993); Jones and Casanova (1993)